SECTION 08 63 00 – REMOVABLE INSULATED TRANSLUCENT FIBERGLASS SANDWICH PANEL STRUCTURAL SKYLIGHT SYSTEM SPECIFICATION

Revise this section by deleting and inserting text to meet project-specific requirements.

Specifier: Consult Structures Unlimited, Inc. for assistance at info@structutresunlimitedinc.com or 1-800-225-3895.

Some specification choices are very involved and require consultation in order for the project’s performance to be as desired by the Owner and Architect.

- GENERAL

      - SUMMARY

        - Section includes the removable structural skylight system as shown and specified. Work includes providing and installing:

          - Structural aluminum box beam superstructure with permanent lifting eye-hooks

          - Factory prefabricated structural insulated translucent sandwich panels

          - Aluminum installation system with exterior accessible anchor bolts

          - Flexible flashing

        - Related Sections:

Insert sections in subparagraph below that contain requirements the Contractor might expect to find in this section but are specified in other sections.

          - <Insert Related Sections>

      - SUBMITTALS

        - Submit manufacturer’s product data. Include construction details, material descriptions, profiles and finishes of components.

        - LEED Submittals:

Retain paragraphs below if LEED V3 or V4 is required.

          - Laboratory test reports for credit SS 7.2: For roofing materials with a Solar Reflectance Index (SRI) for a minimum of 75% of the roof surface of  29 or higher for a steep sloped roof (>2:12) per ASTM E 1980.  Emittance to be greater than .90 per ASTM E 408 or ASTM C 1371.

          - Product Data for Credit MR 4:  Provide documentation demonstrating use of materials with a minimum 10% recycled content (post-consumer + ½ pre-consumer).

          - Provide computer simulation (RADIANCE) that demonstrates that 75% or more of all regularly occupied spaces achieve daylight illuminance levels of a minimum of               25 footcandles (fc) and a maximum of 500 footcandles (fc) in a clear sky condition on Sept. 21 at 9 a.m. and 3 p.m.

        - Submit shop drawings.  Include plans, elevations and details.

        - Submit manufacturer’s color charts showing the full range of colors available for factory finished aluminum.

          - When requested, submit samples for each exposed finish required, in same thickness and material indicated for the work and in size indicated below. If finishes involve normal color variations, include sample sets consisting of two or more units showing the full range of variations expected.

- Select sandwich panel sample size required.

            - Sandwich panels:  [7” x 12”] [14”x28”] units

            - Factory finished aluminum:  5” long sections

        - Submit Installer Certificate, signed by installer, certifying compliance with project qualification requirements.

        - Submit product reports from a qualified independent testing agency indicating each type and class of panel system complies with the project performance requirements, based on comprehensive testing of current products.  Previously completed reports will be acceptable if for current manufacturer and indicative of products used on this project.

Delete product reports below that are not applicable.

          - Reports required (if applicable) are:

            - International Building Code Evaluation Report (AC 177)

            - Flame Spread and Smoke Developed (UL 723)  – Submit UL Card

            - Burn Extent (ASTM D 635)

            - Color Difference (ASTM D 2244)

            - Impact Strength (UL 972)

            - Bond Tensile Strength (ASTM C 297 after aging by ASTM D 1037)

            - Bond Shear Strength (ASTM D 1002)

            - Beam Bending Strength (ASTM E 72)

            - Insulation U-Factor (NFRC 100)

            - NFRC System U-Factor Certification (NFRC 700)

            - Solar Heat Gain Coefficient (NFRC or Calculations)

            - Condensation Resistance Factor (AAMA 1503) (Thermally Broken only)

            - 1200°F Fire Resistance (SWRI)

            - ASTM E1886/1996 or TAS 201, 202 and 203 (Optional-Windborne Debris)

            - Fall Through Resistance (ASTM E 661)

            - Class A Roof Covering Burning Brand (ASTM E 108)

            - (Optional) UL Listed Class A Roof System (UL 790) – Submit UL Card

            - (Optional) LEED Credits

- Please consult with Structures Unlimited, Inc. for Daylighting report to be generated for accurate figures to insert.

        - (Optional) Provide Daylight Autonomy Report showing that the proposed translucent daylighting system will provide <Insert Number> lux in the daylit areas for an average of <Insert Number> % of the daylight hours for the entire year.

      - CLOSEOUT SUBMITTALS

        - Provide project maintenance manuals.

      - QUALITY ASSURANCE

        - Manufacturer’s Qualifications:

          - Material and products shall be manufactured by a company continuously and regularly employed in the manufacture of specified materials for a period of at least ten consecutive years and which can show evidence of those materials being satisfactorily used on at least six projects of similar size, scope and location. At least three of the projects shall have been in successful use for ten years or longer.

          - Panel system must be listed by an ANSI accredited Evaluation Service, which requires quality control inspections and fire, structural and water infiltration testing of sandwich panel systems by an accredited agency.

          - Quality control inspections shall be conducted at least once each year and shall include manufacturing facilities, sandwich panel components and production sandwich panels for conformance with AC177 “Translucent Fiberglass Reinforced Plastic (FRP) Faced Panel Wall, Roof and Skylight Systems” as issued by the ICC-ES.

        - Installer’s Qualifications: Installation shall be by an experienced installer, which has been in the business of installing specified panel systems for at least two consecutive years and can show evidence of satisfactory completion of projects of similar size, scope and type.

      - PERFORMANCE REQUIREMENTS

        - The manufacturer shall be responsible for the configuration and fabrication of the complete removable skylight system, including the aluminum box beam superstructure with lifting eye-hooks.

          - When requested, include structural analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

- Please consult with Structures Unlimited, Inc. to determine the whether the unit will be removed as a complete unit or it will be removed in sections if required due to size.

          - Skylight shall be removable [as a complete unit] [in (enter quantity) sections] by lifting eye-hooks with a crane.  Disassembling individual or small groups of panels does not meet the design intent and is not acceptable.

- Insert structural loads, as determined by project’s structural engineer in subparagraphs below.  Insert all loads in PSF, not wind speed.  If drift load is applicable to the project, provide the necessary profile.

          - Structural Loads; Provide removable skylight system capable of handling the following loads:

            - Roof Live Load, on horizontal projected surface, minimum: <Insert Number> PSF

            - Roof Snow Load, on horizontal projected surface, minimum: <Insert Number> PSF

            - Roof Snow Drift Load, on horizontal projected surface, minimum: <Insert Number> PSF, <Provide Profile>

            - Base Wind Load <Insert Number> PSF factored per applicable Building Code

        - Deflection Limits:

Based on project conditions or requirements of authorities having jurisdiction, more stringent deflection criteria than the specified option in the subparagraphs below may be required.  Building codes include different deflection criteria depending on whether panel assemblies are classified as components and cladding or as part of the main wind-force-resisting system (for example, where a panel assembly is the structural roof).  For discussion of deflection criteria, see "Deflection" Article in the Evaluations in Section 084500 "Translucent Wall and Roof Assemblies."

          - Skylight Panels:  Limited to [l/60] or <Insert Deflection> of clear span.

        - (Optional) Windborne Debris Impact Resistance Performance:

Retain subparagraphs below if required. The International Building Code establishes criteria for buildings in hurricane prone regions. Level of Protection, Wind Zone and Elevation above grade determine required Missile. Insert Missile required, more than one type may be required on a project.

          - Translucent panels must be impact-resistant meeting the requirements of an approved impact-resisting standard: ASTM E 1996 and ASTM E 1886 or TAS 201, 202 and 203.

          - Panel System designed to meet Missile <Insert Missile> per ASTM E 1996.

      - DESIGN

        - Description: Removable Skylight System

- Retain subparagraphs below if information noted below is available. Remove subparagraphs below if information has not yet been finalized. If information is not known, it is best to remove subparagraphs to avoid possible conflicts with the final contract documents.

          - Nominal Size: <Insert Span> x <Insert Length>

          - Aluminum Box Beam Size: [4”x8”] [5”x10”] [6”x13”] [6 3/8”x 16”] [6 3/8”x18”]

          - Roof Pitch: <Insert Angle>

        - Lifting eye-hooks shall be incorporated as required.  Anchor bolts shall be accessed from the outside by removing the perimeter flashing.

      - DELIVERY, STORAGE AND HANDLING

        - Deliver removable skylight system, components and materials in manufacturer’s standard protective packaging.

        - Store removable skylight system panels on the long edge; several inches above the ground, blocked and under cover to prevent warping in accordance with manufacturer’s storage and handling instructions.

      - WARRANTY

Extended Warranties will not apply to all systems, designs, or applications. Please consult Structures Unlimited, Inc.  They may be available depending on project design, scope, location and exposure at additional cost.

        - Provide manufacturer's and installer's written warranty agreeing to repair or replace removable skylight system work, which fails in materials or workmanship within one year from the date of delivery. Failure of materials or workmanship shall include leakage, excessive deflection, deterioration of finish on metal in excess of normal weathering, defects in accessories, insulated translucent sandwich panels and other components of the work.

        - Extended Panel Warranty: <Insert Extended Warranty if required per criteria> years from date of delivery.

        - Extended Manufacturer’s factory applied Finish Warranty: <Insert Extended Warranty if required per criteria> years from date of delivery.

- PRODUCTS

      - MANUFACTURER

        - The basis for this specification is for products manufactured by Structures Unlimited, Inc. Other manufacturers may bid this project provided they comply with all of the performance requirements of this specification and submit evidence thereof.  Listing other manufacturers’ names in this specification does not constitute approval of their products or relieve them of compliance with all the performance requirements contained herein.

        - Structures Unlimited, Inc., Tel: (800) 225-3895 – Fax: (603) 627-0798 – Email: info@structuresunlimitedinc.com

      - PANEL COMPONENTS

        - Face Sheets:

          - Translucent faces: Manufactured from glass fiber reinforced thermoset resins, formulated specifically for architectural use.

            - Thermoplastic (e.g. polycarbonate, acrylic) faces are not acceptable.

            - Face sheets shall not deform, deflect, or drip when subjected to fire or flame.

          - Interior face sheets:

Specify 50 for the standard panel, which meets IBC Class B Interior Finish requirements for most building spaces.

Specify 25 which meets IBC Class A which may be required in unsprinklered, occupied spaces or exitways – see interior finish table in IBC Chapter 8

Specify 25 or less for canopies per IBC 3105.4.

            - Flame spread: Underwriters Laboratories (UL) listed, which requires periodic unannounced retesting, with flame spread rating no greater than [50] [25] [25 or less for canopies] and smoke developed no greater than [250] [350-400 for canopies] when tested in accordance with UL 723.

            - Burn extent by ASTM D 635 shall be no greater than 1”.

          - Exterior face sheets:

Color stability – For standard exterior face: select 5 years exposure.

If for UL Listed Class A Roof or Canopy, Class A sheet face required: select 3 years.

            - Color stability: Full thickness of the exterior face sheet shall not change color more than 3 CIE Units DELTA E by ASTM D 2244 after [3] [5] years outdoor South Florida weathering at 5° facing south, determined by the average of at least three white samples with and without a protective film or coating to ensure long-term color stability. Color stability shall be unaffected by abrasion or scratching.

Projects requiring Windborne Debris Impact Resistance: Retain paragraphs c and d (delete b).

Projects requiring standard impact resistance: Retain paragraphs b and d (delete c).

For paragraph b, the impact strength of the standard .070” thick SW exterior face sheet is 70 ft. lbs.       The optional Hi-Impact face sheet is 230 ft. lbs. which may be required in vandal prone exposures among others. Hi-Impact color is available in white only.

            - Strength: Exterior face sheet shall be uniform in strength, impenetrable by hand held pencil and repel an impact minimum of [70 ft. lbs.] [230 ft. lbs.] without fracture or tear when impacted by a 3-1/4” diameter, 5 lb. free-falling ball per UL 972.

            - (Optional) Strength: Exterior face sheet shall be uniform in strength, with panel meeting ASTM E1996 and ASTM E1886 or TAS 201, 202 and 203.

            - Erosion Protection: Integral, embedded-glass erosion barrier.

          - Appearance:

CAUTION: Face sheet colors affect solar properties. Refer to Light Transmission/SGHC chart.

Exterior face sheets:  Enter thickness and color.

Standard exterior face sheet is .070” thick and is available in standard White or Crystal.

Optional Kal-tints are available in Greenish-Blue, Aqua, Rose and Ice-Blue.

Optional Hi-Impact is .052” thick in White only.

UL Class A roof – Enter .070” thick and is available in standard White Type A or Crystal Type A

Canopy – Enter .070” thick and is available in standard White Type A or Crystal Type A.

Missile D – Enter .060 Hurricane Hi-impact and White in color.

Missile C – Enter .052” Hi-impact and White in color.

Missile A – Enter .070” and White or Crystal (standard colors) or Kal-tints (optional colors)

Interior face sheet: Enter thickness and color.

Standard interior face sheet, either flame spread, is .045” thick and is available in White or Crystal.

Optional Hi-Impact is .052” thick in White only.

            - Exterior face sheet: Smooth, <Insert Thickness> thick and <Insert Color> in color.

            - Interior face sheet:  Smooth, <Insert Thickness> thick and <Insert Color> in color.

            - Face sheets shall not vary more than ± 10% in thickness and be uniform in color.

        - Grid Core:

The grid core may be aluminum or a thermally broken composite of aluminum and fiberglass for maximum thermal efficiency.

Note 1: select Aluminum or thermally broken composite.

Delete note 2 if aluminum I-beam grid core is selected.

          - [Aluminum][Thermally broken composite] I-beam grid core shall be of 6063-T6 or 6005-T5 alloy and temper with provisions for mechanical interlocking of muntin-mullion and perimeter. Width of I-beam shall be no less than 7/16”.

          - I-beam Thermal break:  Minimum 1”, thermoset fiberglass composite.

        - Laminate Adhesive:

          - Heat and pressure resin type adhesive engineered for structural sandwich panel use, with minimum 25-years field use. Adhesive shall pass testing requirements specified by the International Code Council “Acceptance Criteria for Sandwich Panel Adhesives".

          - Minimum tensile strength of 750 PSI when the panel assembly is tested by ASTM C 297 after two exposures to six cycles each of the aging conditions prescribed by               ASTM D 1037.

          - Minimum shear strength of the panel adhesive by ASTM D 1002 after exposure to four separate conditions:

            - 50% Relative Humidity at 68° F: 540 PSI

            - 182° F: 100 PSI

            - Accelerated Aging by ASTM D 1037 at room temperature: 800 PSI

            - Accelerated Aging by ASTM D 1037 at 182° F: 250 PSI

      - PANEL CONSTRUCTION

        - Provide sandwich panels of flat fiberglass reinforced translucent face sheets laminated to a grid core of mechanically interlocking I-beams.  The adhesive bonding line shall be straight, cover the entire width of the I-beam and have a neat, sharp edge.

1. Select 2 ¾” or 4” panels.

2-4. Light Transmission, Solar Heat Gain Coefficient and Panel U-factor are closely linked and must be specified accordingly. Refer to Light Transmission/SHGC Chart.

Furthermore, light transmission needs to be carefully chosen to meet the daylighting expectations of the owner to avoid too much light with resulting unwanted glare and solar heat or too little light to be useful. Kalwall offers a modeling service – See www.DaylightModeling.com, which should be performed and agreed upon prior to final design and specification.

5. Panel U-factors specified are for just the panel itself. The National Fenestration Rating Council has established standardized procedures for comparing fenestration systems based on a complete installed system. View the NFRC Certified Systems values chart for most Kalwall systems. In order to find the appropriate value, specifier must know the properties of the panel specified above as well as the nature of the installation system for the project.

6. Insert Grid nominal size (as viewed) and pattern. Standard grids 12 x 24 shoji, 8 x 20 shoji, or 12” x 12” square pattern called Tuckerman. Custom sizes and patterns available.

          - Thickness: [ 2-3/4”] [ 4”]

          - Light transmission: <Insert Value> %

          - Solar heat gain coefficient:  <Insert Value>

          - Panel U-factor by NFRC certified laboratory: <Insert U-factor >

          - Complete insulated panel system shall have NFRC certified U-factor of: <Insert NFRC U-factor >

          - Grid pattern: Nominal size <Insert Grid Size>; pattern <Insert Pattern>

        - Standard panels shall deflect no more than 1.9” at 30 PSF in 10’-0” span without a supporting frame by ASTM E 72.

        - Standard panels shall withstand 1200° F fire for minimum one hour without collapse or exterior flaming.

        - Thermally broken panels: Minimum Condensation Resistance Factor of 80 by AAMA 1503 measured on the bond line.

The following two paragraphs apply to removable skylight assemblies.

Delete paragraphs E and F if not applicable. Consult IBC or local Code authority for requirements.

Standard removable skylight panels pass Class A Burning Brand.

UL790 Class A Built Up Roof construction is available as an option. Delete line 2 if not required.

        - Removable Skylight System:

          - Removable skylight system shall pass Class A Roof Burning Brand Test by ASTM E 108.

          - (Optional) Roof system shall be UL listed as a Class A Roof by UL 790, which requires periodic unannounced factory inspections and retesting by Underwriters Laboratories.

        - Removable skylight system shall meet the fall through requirements of OSHA 1910.23 as demonstrated by testing in accordance with ASTM E 661, thereby not requiring supplemental screens or railings.

      - BATTENS AND PERIMETER CLOSURE SYSTEM

        - Closure system: Extruded aluminum 6063-T6 and 6063-T5 alloy and temper clamp-tite screw type closure system.

        - Sealing tape: Manufacturer’s standard, pre-applied to closure system at the factory under controlled conditions.

        - Fasteners: Various series stainless steel screws for aluminum closures, excluding final fasteners to the building.

- Insert a color from manufacturer’s standards. Consult with Structures Unlimited, Inc.

        - Finish: Manufacturer's factory applied finish, which meets the performance requirements of AAMA 2604.  Color to be <Insert Color and Number> [selected from manufacturer's standards].

      - SUPERSTRUCTURE

- Select design required for the application – “rigid frame”, “minimal outward thrust” or “truss”.  Consult with Structures Unlimited, Inc. to ensure correct design is selected.

        - The superstructure shall be pre-fabricated of extruded aluminum alloy 6005-T5, 6005A-T61 or 6061-T6 box beams.  Ferrous metals shall not be allowed.  All parts shall be pre-assembled at the factory and knocked down for shipment.  System shall be a <Insert Design> [Rigid Frame] [Minimal Outward Thrust] [Truss] design.

- Insert a color from manufacturer’s standards. Consult with Structures Unlimited, Inc.

        - Finish: Manufacturer's factory applied finish, which meets the performance requirements of AAMA 2604.  Color to be <Insert Color and Number> [selected from manufacturer's standards].

        - Aluminum structural system design and calculations must be furnished in accordance with the Aluminum Association “Specifications for Aluminum Structures” and the applicable building code.  Design calculations must be prepared and stamped by a Licensed Professional Engineer.

        - The superstructure shall incorporate permanent lifting eye-hooks that allow for the unit to be lifted by crane.

- EXECUTION

      - EXAMINATION

        - Installer shall examine substrates, supporting structure and installation conditions.

        - Do not proceed with removable structural skylight installation until unsatisfactory conditions have been corrected by the general contractor.

      - PREPARATION

        - Metal Protection:

          - The general contractor shall prepare foundations, curbs, footings and/or lintels isolating dissimilar materials from aluminum system, which may cause electrolysis.

          - Where aluminum will contact dissimilar metals, protect against galvanic action by painting contact surfaces with primer or by applying sealant or tape recommended by manufacturer for this purpose.

          - Where aluminum will contact concrete, masonry or pressure treated wood, protect against corrosion by painting contact surfaces with bituminous paint or method recommended by manufacturer.

        - The general contractor shall install curbs designed to withstand the thrust generated by the skylight.

        - The general contractor shall provide temporary enclosures required.

      - INSTALLATION

        - Install the removable skylight system in accordance with the manufacturer’s installation recommendations and approved shop drawings.

          - Anchor component parts securely in place by permanent mechanical attachment system.

          - Accommodate thermal and mechanical movements.

        - After other trades have completed work on adjacent material, carefully inspect translucent panel installation and make adjustments necessary to ensure proper installation.

Delete Section 3.4 if not applicable.

      - FIELD QUALITY CONTROL

        - Water Test: Installer to test skylights according to procedures in AAMA 501.2.

        - Repair or replace work that does not pass testing or that is damaged by testing and retest work.

      - CLEANING

        - Clean the skylight system immediately after installation.

        - Refer to manufacturer’s written recommendations.

END OF SECTION 086300